**SECTION 10700**

**ALUMINUM CANOPY**

**PART 1 – GENERAL**

* 1. **SUMMARY**
1. Section Includes: Titan Canopy.
2. Related Requirements: Division 1 – General Requirements

**1.2 REFERENCES**

1. The publications listed below form a part of this specification to the extent referenced. Publications are referenced within the text by the basic designation only.
2. American Welding Society (AWS):
	* 1. Standard D1.2 – Structural Welding Code – Aluminum
3. American Architectural Manufacturers Association (AAMA):
	* 1. Aluminum finishes AAMA 2603 Powder Coat
		2. Aluminum finishes AAMA 2605 Kynar
		3. Aluminum finishes AAMA 611 Anodize
	1. **SUBMITTALS**
4. Submit within 15 days after contract award.
5. Shop Drawings: Indicate size, material and finish. Include plan elevation pages to clearly outline canopy locations. Include installation procedures, details of joints, attachments and clearances. Provide lead time and note possible conflicts where standard line.
6. Color charts showing manufacturer’s full range of colors from standard line.

**PART 2 – PRODUCTS**

* 1. **APPROVED MANUFACTURERS**
1. Specifications are based on Architectural Fabrication, Inc. – Titan Canopy. Architectural Fabrication, Inc. – Manufacturer and Installer is located at 2100 E. Richmond Avenue, Fort Worth, TX 76104. 800.962.8027. [www.arch-fab.com](http://www.arch-fab.com)
2. Substitutions are acceptable assuming they comply with these specifications, are submitted based on Section 01XXX – Substitution Requirements and have a minimum 10 years’ experience.
	1. **MATERIALS**
3. Framing: Aluminum Tube 6063-T52 alloy extruded aluminum.
4. Skin Material: Pre-finished Kynar coated sheet metal by Berridge, MBCI, Pac-Clad or equivalent.
5. Hanger Rods: Zinc plated steel and powder coat. Prime and paint are not acceptable.
6. Connections: Wall plates and canopy mounting brackets are to be aluminum.
7. Hardware and Fasteners: Nuts, bolts, washers, clevis pins, screws, anchors and pipe spacers to be zinc plated or galvanized steel required to suit application and per pre-engineered canopy load requirements.
8. Flashing & Z-Closure: Shall match skin material, fabricated to prevent leakage and sealed with Novaflex metal roof sealant in clear or color match. Other equivalent sealant is acceptable.
9. Finish: Powder coat finish per ASTM D 3451, complying with finish manufacturer’s written instructions for surface preparation including pretreatment, application, baking and minimum dry film thickness. Color to be selected from standard color line.

**PART 3 – EXECUTION**

* 1. FABRICATION
1. Fabricate and preassemble canopies in the shop to greatest extent possible. Disassemble units only as necessary for shipping and handling limitations. Clearly mark units for reassembly and coordinated installation.

**3.2 INSTALLATION**

1. Install canopies per manufacturer’s written instructions and as indicated on drawings.
2. Locate and place canopies level, plumb and at indicated alignment with adjacent work.
3. Use concealed anchors where possible.
4. Repair damaged finishes so no evidence remains of corrective work. Return items to the factory that cannot be refinished in the field. Make required alterations and refinish entire unit or provide new units.
5. Protect galvanized and nonferrous-metal surfaces from corrosion or galvanic action by applying a coating of bituminous paint or elastomeric coating on surfaces that will be in contact with concrete, masonry or dissimilar metals.

**END OF SECTION**